## Slide 1: Non-invasive plasma diagnostics for low temperature deposition of VO2-based thin film by magnetron sputtering (NIDEVO)
Xiao Li
Supervisor: Mgr. Zdeněk Hubička

## Slide 2
Metal–insulator transition (MIT)
Applications: electronic switches, smart coatings, self-cleaning surfaces
insulating monoclinic VO2 (M)
metallic rutile VO2 (R)
T
light
Background: VOx films by reactive HiPIMS （R-HiPIMS）
Challenges
Multiple vanadium oxides (VOx) compounds: VO, VO2, V2O3, V2O5, etc.
Deposition of VOx: Hard to stabilize the process for film growth
Plasma diagnostics
Real-time monitor
Monotonous trend of measured parameter vs QO2
a robust signal with as little scattering as possible

## Slide 3
HiPIMS (High Power Impulse Magnetron Sputtering):
High ionization degree
Dense structure
Smooth surface
R-HiPIMS of VOx: V target+reactive gas (O2)
Difficulties
Hysteresis effect
“Transition”
unstable
“Compound”
stable
“pit on the road”
When does it appear?
Where does it appear?
It shifts as time
But we need it.
Background: VOx films by reactive HiPIMS (R-HiPIMS)
“Metal”
stable

## Slide 4
Method: RF Sobolewski probe
Measured RF current & voltage
Phase shift correction
Sinusoidal RF current and voltage
Sinusoidal RF current 𝒊_𝒔 (𝒕) and voltage 𝒖_𝒔 (𝒕)
Ion flux Γi(t)
Measured RF current & voltage
Phase shift correction
Ion flux Γi(t)
Based on the Sobolewski theory, the ion flux to the substrate Γi(t) is the probe current value at a time when the RF voltage on the space charge sheath around the probe is at the minimum value. 1(RF signal frequency is much lower than the ion plasma frequency)
Ion flux measurement
Γi(t)
and are the filtered RF voltage and current respectively. , and are the average values of and
Sheath impedance （serial mode）
The measured RF current and voltage signals can be transferred to Langmuir-like I–V characteristic curves in the case that the RF probe voltage frequency is much lower than the ion plasma frequency.2
Plasma density ni & electron temperature Te
is ion current density at the floating potential Uf obtained by extrapolation of the ion current part in the I–V curve, is the elementary electron discharge, is the electron density (), is the Bolzman constant, is the mass of Ar, and is the electron temperature in Kelvin
1 M. A. Sobolewski, Appl. Phys. Lett. 72, 1146 (1998).
2 P. Sezemsky et al., Plasma Sources Sci. Technol. 28 (2019) 115009.

## Slide 5
Experiment: invasive probe& non-invasive probe setups
Invasive probe
Non-invasive probe
PHiPIMS = 100 W p = 2 Pa fHiPIMS varies
QAr= 40 sccm τon = 20 µs QO2: 0-2.4 sccm
fRF: 350 kHz
fRF: 350 kHz

## Slide 6
Results: sheath impedance measured at the substrate side
The in-pulse (0-50 µs) and off-pulse (50-725 µs) average imaginary part of sheath impedance value |ImZ|ave,sub to the average cathode current per pulse Ip,ave(sub) ratio, κImZ,sub = |ImZ|ave,sub/Ip,ave(sub) as a function of QO2 obtained at the substrate side.
Slightly smoother trend
Clear trend for R-HiPIMS process control
Clear trend, but not that smooth
κImZ,sub = |ImZ|ave,sub/ Ip,ave(sub)
The in-pulse (0-50 µs), off-pulse (50-725 µs), and full-range (0-725 µs) imaginary part of sheath impedance value |ImZ|ave,sub as a function of QO2 obtained at the substrate side.
Example of the ImZsub(t) curves measured at the substrate side. The zoomed-in in-pulse (0-50 us) and off-pulse (50-725 us) ImZsub(t) curves are inserted as well.

## Slide 7
Results: sheath impedance measured at the target side
The off-pulse (50-800 µs) average value of imaginary part, real part of sheath impedance |ImZ|ave,tar, |ReZ|ave,tar, as well as the total sheath impedance value |Z|ave,tar as a function of QO2 obtained at the target side.
|ImZ|ave&|Z|ave show clear trend
× |ReZ| is not appropriate
κImZ,tar = |ImZ|ave,tar/Ip,ave(tar)
κReZ,tar = |ReZ|ave,tar/ Ip,ave(tar) κZ,tar =
|Z|ave,tar/ Ip,ave(tar)
The off-pulse (50-800 µs) average imaginary part and real part of sheath impedance value |ImZ|ave,tar and |ReZ|ave,tar, as well as the total sheath impedance value |Z|ave,tar to the average current per pulse Ip,ave(tar) ratio, κImZ,tar, κReZ,tar, and κZ,tar as a function of QO2 obtained at the target side.
|ImZ|ave and|Z|ave have close value, no big change of trend
|ReZ| show slightly better trend
Example of the off-pulse (50-800 µs) imaginary part and real part of sheath impedance ImZtar(t), ReZtar(t), as well as the total sheath impedance Ztar(t) curves measured at the target side

## Slide 8
Highlights
Novel non-invasive plasma diagnostics successfully implemented for the deposition process
New discovery of the hysteresis behavior for VOx deposition.
Promising parameter (the sheath impedance, especially the imaginary part of sheath impedance) to locate the transition regime and prepare for future R-HiPIMS process regulation is found.
Results summarized in: X. Li, I. Venkrbcová, D. Lundin, M. Čada, Z. Hubicka, Plasma Sources Science and Technology, 35 (2026) 035003. “Plasma characterization for reactive HiPIMS process regulation of vanadium oxides”. https://doi.org/10.1088/1361-6595/ae4731.

## Slide 9: Thank you for your attention
FZUAVCR
fzu_avcr
institute-of-physics-of-the-czech-academy-of-sciences
fyzikalniustavavcr3220
fzu_avcr
Xiao Li
xiaoli@fzu.cz
www.fzu.cz
Division of Optics (4)
Department of Low-Temperature Plasma (25)
Group of plasma diagnostics and thin film analysis (2505)