## Slide 1: Laser Induced Reactions of p, B and C in a Hollow Target – First Experience

## Slide 2: Contributors:
Inst. of Physics CAS/ELI Beamlines:
J. Řídký, S. Stanček, F. Grepl, A. Velyhan, G. Korn, V. Kantarelou, R. Bičišťová, Y. Levy, J. Huynh, V. Uvarov, P. Hauschwitz, Z. Böhmová, K. Jurek, M. Jarošová
Inst. of Hydrology CAS:
L. Pivokonská, M. Pivokonský, M. Prokopová, K. Sichrová
Inst. of Thermodynamics CAS:
L. Parma, J. Masák, J. Plešek
Inst. of Geology CAS:
L. Ackerman

## Slide 3: Motivation
Richard Magee,
TAE Technologies
Is it possible to start avalanche of pB reactions
provided alphas are produced in a sufficiently
dense environment containing H and B ?
Initial p from Mylar foil
p + 11B  3 α + 8.7 MeV . . . . . 11B 80 %
B-W peaks: ≈ 0.600 MeV, X- sect 0.70 barns
≈ 0.170 MeV, X- sect 0.07 barns

## Slide 4: Motivation
M. Roth and M. Schollmeier
Institute for Nuclear Physics,
Technische Universität Darmstadt
Published by CERN in the
Proceedings of the CAS-CERN
Accelerator School: Plasma Wake Acceleration,
Geneva, Switzerland, 23–29 November 2014,
edited by B. Holzer,
CERN-2016-001

## Slide 5
A multi-MeV alpha particle source via proton-boron
fusion driven by a 10-GW tabletop laser
Valeriia Istokskaia 1,2✉, Marco Tosca 1,3,4, Lorenzo Giuffrida1, Jan Psikal1,2, Filip Grepl1,2, Vasiliki Kantarelou1,
Stanislav Stancek1,5, Sabrina Di Siena6, Arsenios Hadjikyriacou1,2, Aodhan McIlvenny 7, Yoann Levy 8,
Jaroslav Huynh 8, Martin Cimrman 2,8, Pavel Pleskunov3, Daniil Nikitin3, Andrei Choukourov 3,
Fabio Belloni9, Antonino Picciotto10, Satyabrata Kar 7, Marco Borghesi 7, Antonio Lucianetti8,
Tomas Mocek8 & Daniele Margarone https://doi.org/10.1038/s42005-023-01135-x
Laser – Perla B
motivation to use it . . .

## Slide 6: What is a Hollow Target
Filling
this setup allows wide range of materials.
laser beam
In our case:
filling - powders
casing – tungsten,
both cap and container
conductive surface of the cavity
reflects laser pulses inside

## Slide 7: Fillings
Amorphous boron
Rubrene C42H28
melting point: 330-335 °C
boiling point: >315°C

## Slide 8: Target setup
Filling materials:
Empty targets
Rubrene
  pure 100% rubrene
Boron
  pure 100% boron
Rubrene mixed with Boron
  2B:1H ratio
  1B:1H ratio
  1B:2H ratio
  1x Main Frame + 1x Support Holder + 8x target holder

## Slide 9: Experimental setup
IR camera Flir SC7300
Web Cam

## Slide 10: Laser Perla B
used in pulsed mode
20.4 ÷ 21.5 mJ/pulse, freq 100 Hz
1st shot: pre-pulse blocked
pulse duration 1.7 ps
shooting modes: 1, 100, 700 pulses/target
lens protected by debris shield (pellicle)
pellicle #1
empty tungsten targets
pure rubrene
pure boron
pellicle #2
mix boron/rubrene 2B:1H
mix boron/rubrene 1B:1H
mix boron/rubrene 1B:2H
In all cases Mylar foil 0.9 µm placed between cap and container part of the targets

## Slide 11: Laser power during irradiation
transmission of both pellicles measured before and after irradiation
deposit approximated by gaussian
deposit composition and fractions of W, B, (Al) and C measured by SEM
pellicle transmission evolution during irradiation approximated linearly by number of absorbed shots
pellicle # | at. % |  |  | 
 | W | B | Al | C
1 | 0,44 | 2,20 | 0,44 | 96,92
2 | 0,5 | 1,3 | 0,01 | 98,19

## Slide 12: Laser pointing + shooting impact
1 shot traces
in Mylar
Φ ≈ 150 µm
100 (L) and 700 (R) shots traces in Mylar
Φ ≈ 200 µm
1 shot
100 shots
700 shots
impact of shooting at
the bottom of the cavity
in empty tungsten target

## Slide 13
Web Cam view of irradiated targets . . . . 700 shots
W tungsten
Rubrene
Boron
2B:1H
laser frequency is 100 Hz while Web Cam frequency is 23.5 Hz
in average we record 40.8 shots/10 frames

## Slide 14: Results - target after shooting
TOP
BOTTOM
laser beam
this deposit dilutes completely in ultrasound and demi water

## Slide 15: Metamorphosis of the target content
Undiluted content of the cavity (100 shots events)
Rubrene
Boron
2B:1H
9 × 6 µm
50 × zoom →
← 10 × zoom
Brownish grains are unspent rubrene, black grains are unspent B, carbides and various forms of carbon (graphitic carbon - Raman peaks around 1620 cm-1). WO3 is identifiable by Raman peaks. backup slides

## Slide 16: Target temperature – IR camera
We are able to follow temperature time dependence in individual pixels within circumscribed quadrat 15 × 15 pixels with 25 Hz freq.
In the following graphs the max temperature within this quadrat is given.

## Slide 17: Target temperature
If there is only heating by laser (constant)
and simultaneous cooling by heat transfer into target frame and radiation, we will get
by convolution of the two processes the temperature progress in time
. . from the progress of temperature and cooling rate we can reconstruct the progress of heating
by deconvolution

## Slide 18: Target temperature – standard events
B – rubrene 1B:2H in average 13.48 mJ/pulse
Heating:
― by laser
― from deconvolution of measured temperature
― from decon. of measured temperature - 5 frames average

## Slide 19: Target temperature – events with melt
B – rubrene 2B:1H; 100 shots; in average 20.82 mJ/pulse
Heating - slower temperature rise due to melting
Cooling - slow temperature drop as recrystallization releases heat
end of laser shots

## Slide 20: Target temperature – events with peaks
B – rubrene 2B:1H; 700 shots; in average 20.47 mJ/pulse
Heating
slow temp. rise of the whole target; time const ≈ 1.6 sec
fast temp. rise with time const ≈ 0.01 sec; only fraction of the target is heated

## Slide 21: Temperature evolution of target bottom

## Slide 22: Target temperature – events with peaks and melt
B – rubrene 1B:1H; 700 shots; in average 16.99 mJ/pulse
This type of events has
Raman peaks ≈ 1380 and 1620 cm-1 which events with the melt only do not have see backup

## Slide 23: Raman spectra of – events with:
melt and peaks
melt only
non-irradiated amorphous boron

## Slide 24: All events – what we have seen
700 shots events
100 shots events

## Slide 25: 100% Rubrene events - 700 shots
In all events cooling starts immediately after
the last laser shot and
the fit describes the curve entirely – no melt

## Slide 26: Target temperature – pure B + Mylar
B only + Mylar; 100 shots;
in average 13.83 mJ/pulse
end of laser shots

## Slide 27: All events – what we have seen
700 shots events
100 shots events

## Slide 28: WebCam – frame #5
event # | R / B | ∑ sat
f2-t2-n65 | 5.10 | 347 977
f2-t5-n68 | 7.63 | 110 933
f2-t8-n71 | 5.10 | 43 120
event # | R / B | ∑ sat
f3-t2-n29 | X | X
f3-t5-n32 | 0.79 | 359 498
f3-t8-n35 | 0.77 | 416 024
R/B is the ratio of pixels saturated in RED / BLUE saturated pixels

## Slide 29: WebCam – frame #5
event # | R / B | ∑ sat
f1-t8-n62 | 13.38 | 92 262
f1-t5-n59 | 6.66 | 129 751
f1-t1-n55 | 20.33 | 123 589
event # | R / B | ∑ sat
f5-t3-n84 | 0.32 | 586 739
f5-t6-n87 | 0.34 | 679 881
f5-t9-n90 | 0.69 | 1 086 000
R/B is the ratio of pixels saturated in RED / BLUE saturated pixels

## Slide 30: Conclusions
The targets show short local peaks in temperature at certain combinations of laser energy, and B and H density.
We have indication that target filling containing B and H produces plasma with higher temperature.

## Slide 31: Backup slides

## Slide 32: Boron crystallin structure and phase diagram

## Slide 33: Motivation
Negligible contribution of 10B 20 %
p + 10B  7Be + α + 1.1 MeV
p + 11B  3 α + 8.7 MeV . . . . . 11B 80 %
B-W peaks: ≈ 0.600 MeV, X- sect 0.70 barns
≈ 0.170 MeV, X- sect 0.07 barns

## Slide 34: Results - empty targets
1 shot
100 shots
700 shots
empty targets | pure B | pure Rubren | mix R1 B 53.19% | mix R2 B 36.23% | mix R3 B 22.12%
-212.794 | -68.128 | -140.734 | -299.682 | -21.658 | -30.046
-323.531 | -178.019 | -22.748 | -273.788 | -150.193 | -218.294
-380.953 | -108.208 | -53.025 | -253.903 | -29.190 | -132.083
Depth of the dent in tungsten target in µm – 700 shots